## Slide 1: Minerals and waste, an overlooked connection
Mario Tribaudino
Department of Earth Sciences, University of Torino
MINEWA
Minerals and waste, an Anthropocene tale,
Bardonecchia (Torino, Italy) 20-24 June 2022

## Slide 2
Minerals? Fancy crystals?

## Slide 3
The real world
quartz, calcite, clay minerals, iron oxides and hydroxides…
tobermorite, portlandite, monosulphate minerals…

## Slide 4: Minerals, where?
Mining quarrying: minerals as they are, but ground, pulverized, reactions for extraction, reactions in the environment, oxidaytion, bio-mediated reactions
Construction: transformations involving minerals and producing minerals
Manufacturing: production ofmaterial generally unstable at earth condition: some are common minerals, other will become so sooner or later
Waste water: not mineral, but reacts with minerals
Households: not minerals, but the ashes will be

## Slide 5: Minerals, where?
Eurostat: major mineral waste
A lot of the waste from mining and quarrying and from construction and demolition is classified as major mineral waste. Almost three quarter (74 % or 5.2 tonnes per inhabitant) of the total waste generated in the EU in 2018 was major mineral waste.
Major mineral waste
To compare: about 0.5 tonnes per inhabitant MSW

## Slide 6: Minerals where?
Brick composition: 20-30% Al2O3
50-60%SiO2
<5%CaCO3 Fe2O3<5%
Is this enough? Does it explain something?
Like saying human body is 65% o, 18 C, 10H, and minor Ca, P and N.
Bricks are made of minerals:
quartz, feldspar, hematite, mullite, muscovite…
Reactions change with grain size and distribution…
Construction and demolition waste

## Slide 7: Minerals, where?
Seemingly not mineral waste, but, let’s see the processes
Municipal solid waste

## Slide 8: Minerals, where?
Spinels in glassy matrix, with droplets of metal iron
You do not see fancy crystals, but reactions are the same as in natural minerals
What and how to do means something that happens between minerals

## Slide 9: Minerals, why?
Possible reuse and recycling
construction
  concrete
  aggregate
  road pavement
ceramics
recovery of «green» elements
…
Assess performance, show problems, suggest solutions, define geochemical conditions of release and feezing
Geochemical hazard
release of potentially toxic elements (PTE)
powder particles in the air
Typical paths: what is present, how does it react with the environment and in the reuse-recycle conditions

## Slide 10
What is present
The minerals and waste triangle
Which are its properties
What can we do with it
Analytical methods.
Granulometry, OM, XRD, SEM-EDS, ICP-Ms, XRF, TGA, DSC…
Leaching tests, selective extraction, in vitro biological tests…
Chemical an mineralogical composition, texture (grain size and shape, relations with other mineralsgrains)
Reactivity to different chemical and physical stimuli
Development of a new technology product
Performance tests, pre-production breadbord…
Here is most interest

## Slide 11: Minerals, when?
Formed during production
clinker: clay+ CaCO3  C2S, C3S, C3A, C4AF
as minerals named: larnite (C2S belite), hatrurite (C3S alite), not a mineral! (C3A celite), brownmillerite (C4AF)
concrete: cement+aggregate (most minerals)
cement: clinker ettringite (AFt phase), tobermorite (C-S-H), portlandite (CH), (AFm phases, like stratlingite)…
ceramics: caolinite + quartz + feldspar +… glass (not a mineral), quartz, mullite…
MSWI bottom ashes: glass, quartz, portlandite, ettringite, gehlenite…
Formed during weathering
carbonates and sulphates, often soluble
Used as such
aggregate
road embankment
…

## Slide 12: Minerals, what? What is a mineral: geoscience vs waste management
Geoscience
Solid (no water waste)
Inorganic compound (no plastic, no wood)
Crystalline (no glass)
Natural (no waste? no metals?)
Defined composition, in most cases compositional range
Waste management
Solid
Inorganic, but often mingled with organic
Crystalline and amorphous
Seldom natural (e.g. rock aggregate)
Composition and structure same or very similar to natural ones
Mineral names because they are found somewhere in nature

## Slide 13
The same chemical compound, same crystal structure, same reactions, same potential uses, can be or not a mineral according to common definition
Most compounds in waste and in general industrial products have a counterpart in nature, some in exotic rocks
Example: hatrurite, burning of bitumen in a marl
Si (silicon), highly reducing conditions, possible contamination
ettringite
Quarry near Ettringen
cement, delayed ettringite formation
Rare, mineral
Most common, mineral?
In waste management they are all minerals

## Slide 14
An example: glass and crystals in MSWI BA
melilite and glass
Residual glass: original unreacted glass
Newly formed glasses: reactions in local equilibria
white glass
red glass
Minerals, who?

## Slide 15
wollastonite (CaSiO3)
metal Fe
alkali rich glass
Local equilibria in 1x2mm2 grain in bottom ashes from MSWI

## Slide 16
Fe-Ti-Ca oxide
(spinel stoichiometry)
Cu-Sn alloy
glass
Fe oxide
metal Cu
glass
Fe-Ti oxide

## Slide 17: Several glasses and several equilibrium phases

## Slide 18: To end, a geochemical perspective
Comparing continental crust and MSWI BA
The average
The actual distribution
Ca-Si-Al main elements (Si-Al-Fe in CC)
Enriched in Ca and LOI (carbonates, cement minerals…)
High P, organic matter (bones…)
Generally waste follow the same pattern as CC

## Slide 19
Minor elements (less than 1%)
Two groups:
the same (or little less) than continental crust
enriched in waste
Fate:
Forming their own mineral (e.g.NaCl for Cl, CaSO4 for S)
Entering in solid solution

## Slide 20: Where are the minor elements?
The crystal chemical picture is that of oxygen with interstitial space, centered in polyhedra. It is ordered in crystals, disordered in amorphous.
Some elements may be dispersed in crystalline and glassy solid solutions, other form their own phase, other both.
An example, Zn…

## Slide 21: In MSWI BA from Parma, we have found Zn as:
Global Zn is 3200 ppm
Less than 2000 ppm dispersed in glass: solid solution in glass
Solid solution in crystals (spinel 2000-14000 ppm)
Ca[Zn2(OH)6].2H2O
Zn(OH)2

## Slide 22
Conclusions: minerals in waste
Where: minerals are the main constituent of wastes, either in construction and demolition, and in municipal and industrial residues
When: we have minerals from the original rock, inaltered (e.g. concrete aggregate), formed during the industrial processes, or during weathering
What: Definition of minerals in waste management is wider than most accepted in mineralogy: incluses metals, minerals from non natural processes, even if without natural counterpart, and glasses
Who: we can find almost any mineral: common rock forming, like quartz, calcite, feldspars, seldom find in nature like ettringite, very rare in nature, but common in man-made manufactory, like hatruite (C3S), absent in nature like celite or non-mineral, like glass
Why: we want to reuse mineral waste, or recycle in some non-harmful way. Therefore we must know the properties of our minerals.
And now let’s begin!

## Slide 23
Thank you for your attention

## Slide 24: Minerals: when
Natural minerals
mining and quarrying
aggregate in concrete
road pavel
…
Mostly mining and quarrying and construction and demolition wastes